## Slide 1: B.Tech. Project Data Driven Modelling of Composites
End Term Evaluation
Advisor -
Dr. Siladitya Pal
Aman Shrivastava - 13117008
Mihir Ujjwal Rana - 13117044
Yash Sharma - 13117079

## Slide 2: Introduction
Composites -
A composite is a material made from two or more constituent materials with significantly different physical or chemical properties that, when combined, produce a
material with characteristics different from the individual components. The individual components remain separate and distinct within the finished structure. The new material may be preferred for many reasons, primarily to maximize the useful properties and minimize the weaknesses of constituent materials; common examples include materials which are stronger, lighter, or less expensive when compared to traditional materials.

## Slide 3: Applications
Airbus A380
More than 20 % of the A380 is made of composite materials, mainly plastic reinforced with carbon fibres. The design is the first large-scale use of glass-fibre-reinforced aluminium, a new composite that is 25 % stronger than conventional airframe aluminium but 20 % lighter.

## Slide 4: Applications
Automobiles
Composites are being used increasingly in the automotive industry due to their
strength, quality and light-weight. The materials used in automotive engineering play key roles in making lighter vehicles and ultimately lower emissions.

## Slide 5: Applications
Wind Turbine
Currently, carbon fiber is used primarily in the spar, or structural element, of wind blades longer than 45m/148 ft, both for land-based and offshore systems. The higher stiffness and lower density of CF allows a thinner blade profile while producing stiffer, lighter blades.

## Slide 6: Challenges
Since precise material properties are often needed to satisfy industrial needs and criteria, design of composites with tailored properties is of utmost importance.
The design and analysis of such composites faces following challenges -
Computational Expense
Heavy Simulations
Rigorous Experimentation
Time Expensive Process

## Slide 7: Project Objective
To develop an algorithmic framework to predict properties of composites to aid in meta-modelling process.

## Slide 8: Project Timeline

## Slide 9: General Workflow
Random Sequential Adsorption
Images
Image Data Extraction
Master Data
Preprocessed Data
Machine Learning
Trained Model
Predictions
Validation
FEM

## Slide 10: Image Data Extraction

## Slide 11: Image Data Extraction

## Slide 12: Data for Constructing Stress-Strain Curve
The first data set is created for building the stress-strain curves for various composites.
For this, the following features are considered:
  Youngs Moduli of matrix and fibre
  Poisson’s Ratios of matrix and fibre
  Strain (normally distributed; 10 values considered)
  Volume fraction (5%-30%, in increments of 5%)
Characteristics of data:
  Total size (rows) of data = 60,000
  Number of unique materials = 100

## Slide 13: Range of Data Considered

## Slide 14: Results: Stress-Strain Curves at Different Volume Fractions
VF: 5%
VF:10%
VF:15%
R2=0.99
VF = 5%
R2=0.97
VF = 10%
R2=0.96
VF = 15%

## Slide 15: Results: Stress-Strain Curves at Different Volume Fractions
VF:20%
VF:25%
VF:30%
R2=0.95
VF = 20%
R2=0.96
VF = 25%
R2=0.95
VF = 30%

## Slide 16: Random Sequential Adsorption Model
To generate a statistically equivalent RVE, the Random Sequential Adsorption model was used. This method creates a set of randomly distributed distributed points inside a square region, with the constraint that no pair of points may be closer points inside a square region and no closer than a certain minimum distance.
Steps:
Setting the values of volume fraction
Limit the distance between fibres (circles) and between circles and the walls of the unit cell
Required diameter of circles and their number is determined
Required arrangement is obtained in a random manner to ensure isotropic nature

## Slide 17: Finite Element Method
Steps
Generate 5 microstructures for each composite for each volume fraction
  Volume fraction = {0.3, 0.4, 0.5}
  Plane strain (ϵ11, ϵ22, ϵ12)
  Composite range shown on the following slide
Obtain the average stress values
  When L/d > 20, the difference observed due to spatial arrangement of particles is not significant
  L = Length of unit cell, d = diameter of particles
Obtain tangent moduli (formulae shown later)
Feed tangent moduli data to ML model

## Slide 18: Description of Generated Data

## Slide 19: Tangent Moduli Formulae

## Slide 20: Machine Learning
Training
Features:
  Young’s Modulus of Matrix (Em) and Fibre (Ef)
  Poisson’s Ratio of Matrix (νm) and Fibre (νf)
  Volume Fraction (Φ) - obtained from image or set to {0.3, 0.4, 0.5} during generation from FEM
  Tangent Moduli (FEM)
Target:
Tangent Moduli (D1111, D2222, D1212)

## Slide 21: Machine Learning
Algorithms:
  XGBoost Regressor (XGB)
  Random Forest Regressor (RF)
  Ensemble of XGB and RF
After obtaining the tangent moduli, apply relevant formulae (given on next page) to get:
  Young’s Modulus of composite (Em)
  Shear Modulus of composite (D1212)
  Poisson’s ratio of composite (νc)

## Slide 22: Machine Learning Algorithms
Decision Tree
Decision Tree Algorithm
(Graphically)

## Slide 23: Procedure
We considered two composites with properties in our predictable range.
  Glass (Fibre) - Epoxy (Matrix)
    Ef = 71 GPa
    νf = 0.22
    Em = 4 GPa
    νm = 0.35
  Boron (Fibre) - Epoxy (Matrix)
    Ef = 420 GPa
    νf = 0.2
    Em = 4 GPa
    νm = 0.35

## Slide 24: Procedure
Made predictions on 3 different volume fractions
  Volume Fractions (Φ) = 0.3, 0.4, 0.5
Inputs - Em, νm, Ef , νf , Φ

## Slide 25: Procedure
Predictions
  Glass-Epoxy
  Boron-Epoxy

## Slide 26: Accuracy Comparison (Young’s Modulus)

## Slide 27: Percentage Error - Glass Epoxy (Young’s Modulus)

## Slide 28: Accuracy Comparison (Young’s Modulus)

## Slide 29: Percentage Error - Boron Epoxy (Young’s Modulus)

## Slide 30: Conclusions: Findings of the Present Work
A data set comprising nearly 300 different types of materials, when fed to the Machine Learning model, is satisfactorily sufficient in predicting properties of virtually all materials in the range of the data.
Ensembles of several different Machine Learning models tend to perform better than more powerful single models in capturing trends in the data. Furthermore, it also helps in reducing overfitting and building a more robust model.
A Machine Learning approach for constructing the stress-strain curve of a new composite material gives promising results on different materials with different volume fractions, provided the strain is in the range of the data.

## Slide 31: Conclusions: Future Scope
Variation in several other properties of materials like de-bonding of particles/fibres, ductility, and matrix failure (which can be used to calculate toughness and strength) can be introduced.
A more comprehensive database containing information on the manufacturing process of a material, shape, size, etc. can be constructed to enable this data to be used in industry.
Development of faster and automated techniques for generation of composite materials with high volume fractions.
The analysis can be extended to particles/fibres of different diameters.
The analysis can be extended to 3 dimensions with the introduction of particles. However, it would be significantly more computationally expensive.

## Slide 32
Thank You